EXPERIMENTAL INVESTIGATIONS IN DEVELOPING CONCRETE CONTAINING WASTE GLASS POWDER AS POZZOLANA

1 M. N. BAJAD , 2 C.D.MODHERA

1 Department of Civil Engineering, Sinhgad College of Engineering,

Pune- 411041,Maharashtra (India )

2 Department of Applied Mechanics ,Sardar  Vallabhbhai National Institute of   Technology,Surat- 395007,Gujarat( India)

mnbajad@rediffmail.com

ABSTRACT:  Waste glass when ground to a very fine powder shows pozzolanic properties as it contains high SiO2 and therefore to some extent can replace cement in concrete and contribute in strength development. In this paper, an attempt has been made to find out the strength of concrete containing waste glass powder as pozzolana .Cement replacement by glass powder in the range 5% to 40% increment of 5 percentages. (0%, 5%, 10%, 15%, 20%, 25% 30%, 35%, 40%) has been studied. Replacement of 20% cement by glass powder was found to be higher strength

KEY WORDS: Pozzolana, Waste Glass Powder

1. Introduction

Irrespective of the nature of their products, almost all industries produce waste. Effective disposal of wastes therefore is a challenging task. In olden days solid wastes were used as landfills in low-lying areas. Waste disposal in landfill sites however are unsustainable in the long run. Industrial wastes like fly ash, silica fume, blast furnace slag etc. and other wastes of plastics, glass, tiles and agriculture are causing environmental pollution. Recycling of wastes is therefore emerging as an important component of technology for making contribution towards sustainability

Glass is an amorphous solid that has been around in various forms for thousands of years and has been manufactured for human use since 12,000 BCE. The status of glass as a liquid, versus a solid, has been hotly debated. The short story is that glass is a super cooled liquid, meaning that it is rigid and static but does not change molecularly between melting and solidification into a desired shape. Glass is one the most versatile substances on Earth, used in many applications and in a wide variety of forms, from plain clears glass to tempered and tinted varieties, and so forth.

Glass occurs naturally when rocks high in silicates melt at high temperatures and cool before they can form a crystalline structure. Obsidian or volcanic glass is a well known example of naturally occurring glass, although it can also be formed by a lightning strike on a beach, which contains silicate-rich sand. Early forms of glass were probably rife with impurities and subject to cracking and other instability, but examples of glass beads, jars, and eating materials first appeared in ancient Egyptian culture.

When manufactured by humans, glass is a mixture of silica, soda, and lime. Other materials are sometimes added to the mixture to “frost” or cloud the glass or to add color. The elements of glass are heated to 1800° Fahrenheit (982° Celsius). The resulting fused liquid can be poured into molds or blown into various shapes, and wh en cooled, glass is a strong, minimally conducting substance that will not interact with materials stored inside. As a result, glass is frequently used in scientific laboratories to minimize inadvertent chemical reactions and to insulate power lines.

Silica is found in a wide variety of natural sources, including, most commonly, sand. Sodium carbonate, or soda, is used to lower the fusion point of silica, making glass light and workable. Soda is called a flux, because it brings the melting point of the mixture down. Lime is ground from limestone and makes the mixture more viscous, as well as making the glass less susceptible to the erosive qualities of water and acids

Glass is a strange substance, defying easy scientific categorization. It is not a solid, not a gas, and not quite a liquid either. Generally, it is classified as a rigid liquid, maintaining liquid properties while acting like a solid. Heat can return the glass to a liquid and workable form, making it easy to reuse and recycle.

Oldest mouth-blown window-glass in Sweden (Kosta Glasbruk, Småland, 1742). In the middle is the mark from the glassblower's pipe. Pure silica (SiO2) has a "glass melting point"—at a viscosity of 10 Pa·s (100 P)—of over 2300 °C (4200 °F). While pure silica can be made into glass for special applications, other substances are added to common glass to simplify processing. One is sodium carbonate (Na2CO3), which lowers the melting point to about 1500 °C (2700 °F) in soda-lime glass; "soda" refers to the original source of sodium carbonate in the soda ash obtained from certain plants. However, the soda makes the glass water soluble, which is usually undesirable, so lime (calcium oxide (CaO), generally obtained from limestone), some magnesium oxide (MgO) and aluminum oxide (Al2O3) are added to provide for a better chemical durability. The resulting glass contains about 70 to 74% silica by weight and is called a soda-lime glass. Soda-lime glasses account for about 90% of manufactured glass.

Most common glass has other ingredients added to change its properties. Lead glass or flint glass, is more 'brilliant' because the increased refractive index causes noticeably more "sparkles", while boron may be added to change the thermal and electrical properties, as in Pyrex. Adding barium also increases the refractive index. Thorium oxide gives glass a high refractive index and low dispersion and was formerly used in producing high-quality lenses, but due to its radioactivity has been replaced by lanthanum oxide in modern eye glasses. Large amounts of iron are used in glass that absorbs infrared energy, such as heat absorbing filters for movie projectors, while cerium(IV) oxide can be used for glass that absorbs UV wavelengths.

Another common glass ingredient is "cullet" (recycled glass). The recycled glass saves on raw materials and energy. However, impurities in the cullet can lead to product and equipment failure.

Finally, fining agents such as sodium sulfate, sodium chloride, or antimony oxide are added to reduce the bubble content in the glass. Glass batch calculation is the method by which the correct raw material mixture is determined to achieve the desired glass composition.

There are three classes of components for oxide glasses: network formers, intermediates, and modifiers. The network formers (silicon, boron, and germanium) form a highly cross-linked network of chemical bonds. The intermediates (titanium, aluminum, zirconium, beryllium, magnesium, zinc) can act as both network formers and modifiers, according to the glass composition. The modifiers (calcium, lead, lithium, sodium, potassium) alter the network structure; they are usually present as ions, compensated by nearby non-bridging oxygen atoms, bound by one covalent bond to the glass network and holding one negative charge to compensate for the positive ion nearby. Some elements can play multiple roles; e.g. lead can act both as a network former (Pb4+ replacing Si4+), or as a modifier.

The presence of non-bridging oxygen’s lowers the relative number of strong bonds in the material and disrupts the network, decreasing the viscosity of the melt and lowering the melting temperature.

The alkaline metal ions are small and mobile; their presence in glass allows a degree of electrical conductivity, especially in molten state or at high temperature. Their mobility however decreases the chemical resistance of the glass, allowing leaching by water and facilitating corrosion. Alkaline earth ions, with their two positive charges and requirement for two non-bridging oxygen ions to compensate for their charge, are much less mobile themselves and also hinder diffusion of other ions, especially the alkalis. The most common commercial glasses contain both alkali and alkaline earth ions (usually sodium and calcium), for easier processing and satisfying corrosion resistance. Corrosion resistance of glass can be achieved by dealkalization, removal of the alkali ions from the glass surface by reaction with e.g. sulfur or fluorine compounds. Presence of alkaline metal ions has also detrimental effect to the loss tangent of the glass, and to its electrical resistance; glasses for electronics (sealing, vacuum tubes, lamps...) have to take this in account.

Addition of lead(II) oxide lowers melting point, lowers viscosity of the melt, and increases refractive index. Lead oxide also facilitates solubility of other metal oxides and therefore is used in colored glasses. The viscosity decrease of lead glass melt is very significant (roughly 100 times in comparison with soda glasses); this allows easier removal of bubbles and working at lower temperatures, hence its frequent use as an additive in vitreous enamels and glass solders. The high ionic radius of the Pb2+ ion renders it highly immobile in the matrix and hinders the movement   of other ions; lead glasses therefore have high electrical resistance, about two orders of magnitude higher than soda-lime glass (108.5 vs 106.5 Ohm·cm, DC at 250 °C). For more details, see lead glass.

Addition of fluorine lowers the dielectric constant of glass. Fluorine is highly electronegative and attracts the electrons in the lattice, lowering the polarizability of the material. Such silicon dioxide-fluoride is used in manufacture of integrated circuits as an insulator. High levels of fluorine doping lead to formation of volatile SiF2O and such glass is then thermally unstable. Stable layers were achieved with dielectric constant down to about 3.5–3.7.      The amorphous structure of glassy Silica (SiO2) in two dimensions. No long range order is present, however there is local ordering with respect to the tetrahedral arrangement of Oxygen (O) atoms around the Silicon (Si) atoms.The    standard definition of a glass (or vitreous solid) is a solid formed by rapid melt quenching. If the cooling is sufficiently rapid (relative to the characteristic crystallization time) then crystallization is prevented and instead the disordered atomic configuration of the supercooled liquid is frozen into the solid state at the glass transition temperature Tg. Generally, the structure of a glass exists in a metastable state with respect to its crystalline form, although in certain circumstances, for example in atactic polymers, there is no crystalline analogue of the amorphous phase. As in other amorphous solids, the atomic structure of a glass lacks any long range translational periodicity. However, due to chemical bonding characteristics glasses do possess a high degree of short-range order with respect to local atomic polyhedra. It is deemed that the bonding structure of glasses, although disordered, has the same symmetry signature (Hausdorff-Besicovitch dimensionality) as for crystalline materials

Utilization of waste glass is very important for human development because

1.	Huge amount of glass waste produce by human increases the need of land to       get rid

2. Use up precious landfill space, decreasing possible area that can be used for landfills of other waste increasing the need to establish new expansive landfills

3.  lactates and gas releases from the   landfill site degrade communities living condition and harmful to human health

4	location of most recycling plants are built within low income neighborhoods because of cheap labor and strict regulation may affect respiratory system if breath in pollutants. Case-local residents at Mercedes Arumbula claimed that the neighborhood and kids have developed asthma once the plant was built in their community

5.	Glass is non-biodegradable (remains in our environment and do not decompose easily by itself therefore do not have significant environmental and social impact could result in serious impact after disposal.

2.Literature review

The concrete industry has been making use of industrial wastes like fly ash, silica fume and blast furnace slag as pozzolana by replacing a part of cement.1 While Pozzolanic reaction adds to the strength of concrete and the utilization of these materials brings about economy in concrete manufacture.     It has been estimated that several million tons of waste glasses are generated annually world wide2. The key sources of waste glasses are waste containers, window glasses, windscreen, medicinal bottles, liquor bottles, tube lights, bulbs, electronic equipments, etc. Only a part of this waste glass can be recycled. A majority of the waste glass remains unutilized.

Table 1: Oxide content for waste glass powder.

| Oxide | Content (%) |
| --- | --- |
| SiO2 | 72 |
| Na2O | 14 |
| CaO | 9 |
| Al2O3 | 2 |
| MgO | 2.2 |
| K2O | 0.5 |
| Fe2O3 | 0.2 |
| Cr, S, and Co | 0.1 |

Waste glass is a major component of the solid waste stream in many countries and is generally used in landfills3. As an alternative, however, waste glass could be used as a concrete aggregate, either as a direct replacement for normal concrete aggregates (low value) or as an exposed, decorative aggregate in architectural concrete products (high value). Expansive alkali silica reactions (ASR) can occur between glass particles and cement paste, particularly in moist conditions and high alkali cements. This reaction can occur whenever aggregates contain reactive silica. However it is now well known that by controlling cement alkali level and moisture, the reaction can be mitigated 4,6. Research has shown that the waste glass can be effectively used in concrete either as aggregate or as pozzolana. Waste glass when ground to a very fine powder shows pozzolanic properties. Therefore glass powder shows pozzolanic properties. Therefore glass powder can partially replace cement and contribute to strength development.

Finely ground glass has the appropriate chemical composition including SiO2 to react with alkalis in cement (Pozzolanic Reaction) and form cementitious products that help contribute to the strength development5. Alkali silica reaction (ASR) of glass aggregate concrete can be minimized by the use of the suppressants including pulverized fuel ash (PFA) and metakaolin (MK)2.

3. Research Significance

Recycling of waste glass possesses major problems for municipalities everywhere, and this problem can be greatly eliminated by re-using waste glass as cement replacement in concrete. Moreover, there is a limit on the availability of natural aggregate and minerals used for making cement, and it is necessary to reduce energy consumption and emission of carbon dioxide resulting from construction processes, solution of this problem are sought thought usages of waste glass as partial replacement of Portland cement. Replacing cement by pozzolanic material like waste glass powder in concrete, not only increases the strength and introduces economy but also enhances the durability. Chlorides and sulphates of sodium, magnesium and calcium are present in alkaline soils and water. Sulphates react chemically with product of hydration causes expansion and chloride deposited in the concrete that tend to make the concrete more porous .Therefore, the action of chlorides and sulphates in concrete containing waste glass powder needs to be investigated

4. Experimental Programme

In this experimentation an attempt has been made to find out the strength of concrete produced by replacing the cement with waste glass powder in various percentages ranging from 5% to 40% in increments of 5% (0%, 5%, 10%, 15%, 20%, 25%, 30%, 35%, 40%)

Ordinary Portland Cement (OPC) 43 grade, locally available sand and coarse aggregates were used in this experiments. The sand used was a Zone II had the specific gravity of 2.62. The specific gravity of the coarse aggregate was 2.93. The coarse aggregate used were of 12 mm and down size. To impart workability to the mix, a superplasticiser from a reputed company was used with the dosage of 1% by weight of cement. The glass powder was obtained by crushing waste glass pieces in a cone crusher mill. The 600 micro passing fraction was used for the experimentation. Chemical composition of glass powder is shown in Table 1

Table 2: Results of compressive strength for 30 days.

Mix design carried out for M20 grade of concrete by IS 10262:1982, yielded a mix proportion of 1:1.34:3.2 with a water cement ratio of 0.4539.Specimens were prepared according to the mix proportion and by replacing cement with glass powder in different proportion. To find out the Compressive strength, specimens of dimensions 150X150X150mm were cast and tested using a compressive testing machine (CTM) of capacity 2000KN as per IS 516:195940

5.Test results

Table2,3 and Figures1,2 show the results of compressive strength of concrete with glass powder in cement in different proportions over 30 and 90 days

Table 3: Results of compressive strength for 90 days.

| Percentage replacement of cement by glass powder (%) | Compressive Strength (MPa) | Percentage increase or decrease in compressive strength w.r.f. ref.mix. |
| --- | --- | --- |
| 0 | 27.33 | - |
| 5 | 28.87 | +6 |
| 10 | 30.08 | +10 |
| 15 | 31.85 | +17 |
| 20 | 33.86 | +24 |
| 25 | 30.82 | +13 |
| 30 | 24.44 | -11 |
| 35 | 22.72 | -17 |
| 40 | 19.25 | -30 |

6. Discussion on test results

| Percentage replacement of cement by glass powder (%) | Compressive Strength (MPa) | Percentage increase or decrease in compressive strength w.r.f. ref.mix. |
| --- | --- | --- |
| 0 | 27.05 | - |
| 5 | 28.58 | +6 |
| 10 | 29.77 | +10 |
| 15 | 31.56 | +17 |
| 20 | 33.50 | +24 |
| 25 | 30.52 | +13 |
| 30 | 24.22 | -10 |
| 35 | 22.44 | -17 |
| 40 | 19.03 | -30 |

An increasing trend in compressive strength was observed with increasing replacement of cement with glass powder up to 20%. The highest percentage increase in the compressive strength was about 24% and 20% replacement level. When the cement replacement level was increased beyond 20%, the compressive strength decreased.

The increase in strength up to 20% replacement of cement by glass powder may be due to the pozzolanic reaction of glass powder. Also it may be due to the glass powder effectively filling the voids and giving rise to dense concrete microstructure. However, beyond 20% the dilution effect takes over and the strength starts to drop. Thus it can be concluded that 20% was the optimum level for replacement of cement with glass powder.

Conclusions

Based on experimental observations, higher strengths were achieved when 20% cement was replaced by glass powder in concrete

References

- Suryanshi.C.S., “Use of industrial and domestic waste in concrete”, Civil Engineering and Construction Review,26(Februrary1999)pp-26-31.

- Byars E.A.,Morales.B. and Zhu H.Y., “ Waste glass as concrete aggregate and pozzolana-laboratory and industrial projects”,Concrete,38(January2004,)pp41-44.

- Byars E.A.,Zhu H.Y. and Morales B. , Conglasscrete I ,www.wrap.org.uk

- Baxer.s, Jin W and Meyer C., “Glasscrete-Concrete with glass aggregate,ACI Materials journal,march-April2000,pp208-213.

- Tang Albert,Dhir Ravindra,Dyer,Tom and Yongjun, “Towards maximizing the value and sustainable use of glass”, Concrete Journal,38(Journal 2004),pp38-40.

- Byars E.A.,Zhu H.Y. and Morales B., ConglasscreteII,www.wrap.org.uk

- Seung Bum Park, Bong chum Lee and Jeong Hwan Kim., “Studies on mechanical   properties of concrete containing waste glass aggregate”, Cement and concrete Research 34(2004),pp.2181-2189.

- Omer ozkand and Isa Yuksel, “ Studies on mortars containing waste  bottle glass and industrial  by-products”,Construction and Building Materials 22(2008),pp1288-1298.

- Nathan Schwarz, Hieu cam and Narayanan Neithallath, “ Influence of a fine glass powder on the durability characteristics of concrete and its comparison to fly ash”,Cement and   Concrete Composites 30(2008),pp486-496.

- C.H. Chen,R.Huang,J.K.Wu and C.C.Yang. , “ Waste E-glass particles used in cementitious mixtures”,Cement and concrete Research 36(2006) ,pp-449-456.

- Her-Yung Wang, “A Study of the effects of LCD glass sand on the properties of concrete”,Waste Management 29(2009), pp-335-341.

- Jitendra A.Jain and Narayanan Neithalath, “ Chloride transport in fly ash and glass powder modified concrets-Infludence of test methods on microstructure”.,Cement and Concrete Composites 32(2010),pp148-156.

- Nathan Schwarz and Narayanan Neithalath “Influence of a  fine glass powder on cement hydration: comparison to fly ash and modeling the degree of hydration”,Cement and Concrete Research 38(2008).,pp429-436.

- Yixin Shao,Thibaut Lefort,Shylesh Moras and Damian Rodriguez, “Studies on concrete containing ground waste glass”,Cement and Concrete Research 30(2000).,pp91-100.

- L.M.Federico and S.E.Chidiac, “ Waste glass as Supplementary Cementitious material in concrete-Critical review of treatment methods”Cement and Concrete Composites 31(2009).,pp606-610.

- R.S.Bang,I.K.Pateriya and M.R. Chitalange, “ Use of pond ash as fine aggregate-Experimental Study”,New Construction Materials,Jan.2009.,pp48-51.

- Manjit Singh,Mridul Garg and   K.K.Somani., “Experimental investigations in   developing low cost masonry cement from industrial wastes”, The Indian Concrete Journal,March(2006),pp31-36.

- M.A.Rashid,Tanvir Hossain and M.Ariful Islam “Higher Strength   concrete   using crushed brick as coarse aggregate The Indian Concrete Journal.,Oct.(2008).,pp18-23.

- A.Guerrero,M.S.Hernandez and S.Goni., “ The role of the fly ash pozzolanic activity in Simulated Sulphate radioactive liquid waste”.,Waste Management 20(2000)51-58.

- Seung-Bum   Park and Bong-Chum Lee, “Studies on expansion properties in mortar containing waste glass and fibers” CementS and Concrete Research 34(2004),pp1145-1152.

- Yun-Wang Choi,Dae-Joong Moon,Jee-Seung Chung and Sun-Kyu Cho, “ Effects of waste PET bottles aggregate on the properties of concrete”, Cement and Concrete Research 35(2005).,pp776-781.

- P.T.Santosh Kumar, “ Combined influence of sand and water cement ratio on the compressive strength of concrete”,The Indian Concrete Journal,Sept.(2009).,pp9-14.

- Caijun Shi,Yanzhhhong Wu,Chris Riefler,and Hugh Wang, “ Characteristics and pozzolanic reactivity of glass powders”, Cement and Concrete Research 35(2005).,pp987-993.

- Bashar Taha and Ghassan Nounu, “ Using Lithium nitrate and pozzolanic glass powder in concrete as ASR Suppressors”, Cement and Concrete Composites 30(2008).,pp497-505.

- Mukesh   C.Limbachiya, “ Bulk engineering and durability properties of washed glass sand concrete”,Construction and Building Materials 23(2009).,pp1078-1083.

- Andrea Saccani and Maria chiara Bignozzi, “ASR expansion behavior of recycled glass fine aggregates in concrete”,Cement and Concrete Research 40(2010).,pp531-536.

- Rachida Idir,Martin Cyr and Arezki Tagnit-Hamou., “  Use of fine glass as ASR inhibior in glass aggregate mortars”, Construction and Building Materials 24(2010).,pp1309-1312.

- V.Ducman, A.Mladenovic and J.S.Suput“Lightweight aggregate based on waste glass and its alkali-Silica reacitivity”, Cement and Concrete Research 32(2002).,pp223-226.

- Her-Yung Wang and Wen-Liang Huang ., “ A Study on the properties of fresh self- consolidating glass concrete(SCGC)”,Construction and Building Materials 24(2010).,pp619-624.

- Mohamad J.Terro, “ Properties of concrete made with recycled crushed glass at elevated temperatures”, Building and Environment 41(2006).,pp633-639.

- Ahmad Shayan and Aimin Xu, “ Performance of glass powder as a pozzolanic material in concrete: A field trial on concrete slabs”,Cement and Concrete Research 36(2006),pp547-468.

- M.Shahul Hameed and A.S.S.Sekar, “ Quarry dust as replacement of fine aggregates in concrete”, New construction Materials,Jan(2009),pp52-56.

- Ilker Bekir Topcu and Mehmet Canbaz, “Properties of Concrete Containing Waste glass”, Cement and Concrete Research 34(2004),pp267-274.

- Bashar Taha and Ghassan Nonu, “Properties of Concrete contains mixed colour waste recycled glass as sand and cement replacement”, Construction and Building Materials 22(2008),pp731-720.

- M.S.Shetty, “Concrete Technology Theory and Practice”S.Chand and Company Ltd.,New Delhi,2006.

- M.L.Gambhir, “ConcreteTechnology”,Tata McGRAW-Hill Publishing Company Limited,New Delhi,2006.

- H.Sood,L.N.Mittal, P.D. Kulkarni, “Laboratory Manual on Concrete Technology”,CBS Publishers and Distributors, New Delhi,2003.

- -------------Indian Standard code of practice for plain and Reinforced Concrete, IS456:2000,Bureaue of Indian Standards, New Delhi.

- -------------Recommended  guidelines of concrete mix design, IS 10262:1982, Bureau of Indian Standards, New Delhi.

- -------------Method of tests for strength of concrete, IS 516:1959, Bureau of Indian Standards, New Delhi.

- --------------Splitting tensile strength concrete method of test, IS5816:1999, Bureau of Indian Standards, New Delhi.